## Slide 1: Environmental Scanning Electron Microscope (ESEM)

## Slide 3: Environmental Scanning Electron Microscope
Imaging Voltage: 10Kv- 30kV
Modes:
High Vacuum Mode
Low Vacuum Mode
Environmental Mode (ESEM mode)

## Slide 4: High Vacuum Mode
Detector: Everhart Thornley Detector (ETD)
Vacuum range - below 4.5e-4 Pa
Sample :
Conducting
Non conducting sample can be coated and observed

## Slide 5: Fractrography and cutting tools Fractography of corroded CT Four fluted micro end mill

## Slide 6: Biological Samples Red Blood cells Plant leaf structure
Sample are non-conducting and coated

## Slide 7: Scaffold Fossil
Sample are non-conducting and coated

## Slide 8: Low Vacuum Mode
Detector: Large Field Detector (LFD)
Pressure range: 10-130 Pa
Sample :
Non- Conducting
Un-coated

## Slide 9: Flower Fish scales
Sample are non-conducting and un coated
Low vacuum mode

## Slide 10: ESEM Mode
Detector: Gaseous Secondary Electron Detector (GSED)
Pressure range 130 – 4000 pa
Peltier stage
Sample :
Wet and Moist samples

## Slide 11: Ant Water droplets on butterfly wing
Sample are non-conducting and coated
ESEM

## Slide 12: Back Scattered Imaging
Detector: Solid State Detector (SSD)
Used in High Vacuum and Low Vacuum Mode
Topological and Compositional contrast can be observed
Sample :
Conducting
Non- Conducting

## Slide 13: Back Scattered Imaging
Rock-pyrites
AlZr fibers

## Slide 14: Energy Dispersive X-ray Spectroscopy (EDS)
Chemical characterization of sample.
Each element has a unique atomic structure allowing unique set of peaks on X ray spectrum
The number and energy of X ray emitted is measured by EDS.

## Slide 15: EDS analysis

## Slide 16: Selected area EDS with Quantification

## Slide 17: Mapping and line analysis
X-ray mapping provides images of elemental distribution in a sample.
Different phases in a material can studied
X- ray maps are produced by recording number of X ray photons of a specified energy generated from each point over a fixed counting time while the electron beam is rastered over a rectangular area.

## Slide 18: Mapping Sample: Al-Sn alloys

## Slide 19: Line analysis
Chromium carbide - Nickel chromium coating on Mild steel substrate

## Slide 20
Thank you.