## Slide 1: DUAL BEAM – FOCUSED ELECTRON AND ION BEAM

## Slide 4
Lamella Preparation, Thinning and STEM imaging using FIB at SAIF
Sample : Interstitial steel
Required information : To study grains and grain boundaries in the sample

## Slide 5
Lamella analysis using TEM Imaging and EDS Characterization (HR-TEM 300 kV, Tecnai G2, F30 at SAIF)

## Slide 6
Lamella Preparation, Thinning and STEM imaging and EDS analysis using FIB at SAIF
Sample : TiO2/SiO2
Required information : To study alternate multilayers of TiO2 and SiO2

## Slide 7
STEM imaging and EDS analysis using FIB at SAIF

## Slide 8
Lamella Preparation, Thinning and STEM imaging and EDS analysis using FIB at SAIF
Sample 3 : Ni on Pyramidal Si
Required information : To check if oxide is present at the Ni - Si interface

## Slide 9
Nano Patterning on Au using FIB
Micro rings and holes on Titanium
NANO PATTERNING for Optical lenses on gold and Titanium

## Slide 10
Tin balls on Carbon
Au on Ag Nano Forest
Mesoporous Silica
Au on Carbon
IMAGE ANALYSIS on the Dual beam-FIB at SAIF